Product Information

Product Name: Dark gray Masterbatch

Product Code:01-2390-04

Carrier Resin: PE

Masterbatch Type: Opaque

Proper to use in: poly olefins

Description: Dark gray Masterbatch is designed to mix with Polyethylene and Polypropylene to use for injection molding, blow molding and… .

Benefits: It’ll be completely solved in polymer. When the granules are mixed with polymer matrix and it has been molded, the final production has bright and shiny dark gray color

Technical Data

Heat Stability: 240°C

Use this masterbatch in 1% of weight.

Dark gray Masterbatch includes mineral filler.

Keep this product in dry place below 40° Centigrade

 Tel: 021-56572878-9 [www.payonpolymer.com](http://www.payonpolymer.com)

 Tel fax: 021-56572880 info@[www.payonpolymer.com](http://www.payonpolymer.com)